# SSS Sintering Process

1a2a: Heated in furnace from room temperature  970 °C.

2a3a: Sintered overnight for ~16 hours in air.

3a4a: Cooled to room temperature in flowing oxygen over a ~7-8 hour period.

# MPMG Sintering Process

1b2b: Heated in furnace from room temperature  1070°C @ 10°C/min.

2b3b: Held at 1070°C for 30 min. Cooled from 1070°C  1000°C @ 1.17°C/min.

3b4b: Cooled from 1000°C  950°C @ 1°C/hr

4b5b: Cooled from 950°C  room temperature over weekend at natural furnace cooling rate

6b7b: Heated to 600°C for 30 min.

7b8b: Furnace cooled overnight in presence of oxygen gas stream @ 8mL/min.